## Slide 1: Beyond atomistics: large scale atomistic fracture simulations in pyiron

## Slide 2: K-controlled “Pacman” crack configurations
Simulations to determine (anisotropic) fracture toughness ()
Displacement field according to linear anisotropic elastic solution under plane strain condition
Radius of configurations should be large enough to converge with infinite limit of linear elastic fracture mechanics
Quasi-2D configurations usually contain 100k – 2M atoms
Study of crack front effects (3rd dimension) can multiply number of atoms by a factor of 10 or more
Düsseldorf - pyiron hackathon 2024
Tara
Atomically sharp crack
Disp. field
Boundary layers (red atoms) fixed
(Normal to crack plane) Y
X (Propagation dir.)
(Crack front dir.) Z
fcc
unidentified
Adaptive CNA:

## Slide 3: Loading procedure
Incremental (“quasistatic”) loading – minimization using FIRE
Typically 5 – 100 iterations for sharp cracks (average 50)
Düsseldorf - pyiron hackathon 2024
Tara
Atomically sharp crack
Identify load at which crack is stable at center: Kin
Crack propagates:
sufficiently small
Möller and Bitzek, MSMSE, 2014
  8 potentials (Fe)
  6 crack systems
  Approx. 2400 calculations
Hiremath et al., Comp. Mat. Sci., 2022
  9 potentials (W)
  9 crack systems
  Approx. 4050 calculations
Wu and Curtin, Acta Mater., 2015
  1 potential (Mg)
  9 crack systems
  3 small blunting radii
  Approx. 1350 calculations

## Slide 4: Influence of crack tip radius on fracture toughness of blunted cracks
Displacement field according to linear anisotropic elastic solution under plane strain condition
Düsseldorf - pyiron hackathon 2024
Tara
Blunted crack
Disp. field
Remove atoms
(Normal to crack plane) Y
X (Propagation dir.)
(Crack front dir.) Z
Atomically sharp crack
Disp. field
Boundary layers (red atoms) fixed
(Normal to crack plane) Y
X (Propagation dir.)
(Crack front dir.) Z

## Slide 5: Loading procedure
Incremental (“quasistatic”) loading – minimization using FIRE
Blunting increases number of iterations to fracture
Düsseldorf - pyiron hackathon 2024
Tara
Atomically sharp crack
Identify load at which crack is stable at center: Kin
Crack propagates:
sufficiently small
Blunted crack
Start at Kin identified for sharp crack
Sharp crack re-initiates:
sufficiently small

## Slide 6: High-throughput nature
Blunting increases number of iterations to fracture
Large blunting increases necessary radius of configurations
2 crack systems, 2 harmonic potentials, average 200 iterations each: 6800 calculations
Düsseldorf - pyiron hackathon 2024
Tara
Name | Radius as layers removed | 5/2 | 5/2 | 5/2 | 5/2
Size (Approx.) |  | 75K atoms | 300K atoms | 1.2M atoms | 2.7M atoms
sharp | 0 | 1.58 (-) | 1.60 (1.27%) | 1.61 (0.63%) | -
blunt r01 | 1 | 1.65 (-) | 1.65 (0%) | - | -
blunt r03 | 3 | 1.99 (-) | 1.97 (1.01%) | - | -
blunt r09 | 9 | 2.87 (-) | 2.73 (4.88%) | 2.67 (2.20%) | -
blunt r18 | 18 | - | 3.78 (-) | 3.58 (5.29%) | 3.54 (1.12%)
blunt r27 | 27 | - | 4.75 (-) | 4.36 (8.21%) | 4.25 (2.52%)
Name | Radius as layers removed |  |  |  | 
Size (Approx.) |  | 75K atoms | 300K atoms | 1.2M atoms | 2.7M atoms
sharp | 0 | 1.58 (-) | 1.60 (1.27%) | 1.61 (0.63%) | -
blunt r01 | 1 | 1.65 (-) | 1.65 (0%) | - | -
blunt r03 | 3 | 1.99 (-) | 1.97 (1.01%) | - | -
blunt r09 | 9 | 2.87 (-) | 2.73 (4.88%) | 2.67 (2.20%) | -
blunt r18 | 18 | - | 3.78 (-) | 3.58 (5.29%) | 3.54 (1.12%)
blunt r27 | 27 | - | 4.75 (-) | 4.36 (8.21%) | 4.25 (2.52%)

## Slide 7: The Workflow: coarse-grained macro view
Düsseldorf - pyiron hackathon 2024
Tara
Theoretical (Griffith) fracture toughness () - Analytical
Load at which crack is stable () - simulated
Load at which crack tip bond breaks () - simulated
Surface energy
Initial guess for identifying load
Starting load for incremental loading
Create cylinder without crack
Elastic constants
Crystal parameters

## Slide 8: Theoretical fracture toughness: fine-grained node view
Düsseldorf - pyiron hackathon 2024
Tara
Rotate to orientation
Analytical calculation
Surface energy
Elastic constants
Orientation
Theoretical load

## Slide 9: Cylinder creator: fine-grained node view
Düsseldorf - pyiron hackathon 2024
Tara
Generic structure creator
Cut cylinder
Radius
Lattice constant
Orientation
Cylindrical structure (no crack)
Crystal structure type
Centre coordinates

## Slide 10: Stable crack: fine-grained node view
Düsseldorf - pyiron hackathon 2024
Tara
Displacement field (to introduce crack)
Energy Minimizer
Convergence criteria
Cylindrical structure (no crack)
Orientation
Output structures
Elastic constants
Algorithm(s) choice
Boundary layer thickness
(Non-) Periodic boundaries
for loop over load range
Load

## Slide 11: Incremental loading: fine-grained node view
Düsseldorf - pyiron hackathon 2024
Tara
Displacement field (to increase load on crack)
Energy Minimizer
Convergence criteria
Output structures
Algorithm(s) choice
Boundary layer thickness
(Non-) Periodic boundaries
for loop over load range
Stable crack structure
Orientation
Elastic constants
Load
Only to start loading process

## Slide 12: Visualization: Common Neighbour Analysis (CNA)
Düsseldorf - pyiron hackathon 2024
Tara
Crack system (100)[011]
blunt-r01
blunt-r16
sharp
blunt-r04
Crack system (100)[001]
blunt-r01
blunt-r16
sharp
blunt-r04
y
x
z
fcc
hcp
unidentified
Adaptive CNA:
bcc
y
x
z
In many cases of studying qualitative fracture behaviour, the atoms of native crystal structure type can be hidden (e.g., Tungsten - bcc)
But those atoms may be important to study e.g., twins

## Slide 13: Visualization: Stress field analysis
Düsseldorf - pyiron hackathon 2024
Tara
Usually, the atomistic stresses are important only along the crack plane.
But even otherwise, the stresses only need to be visualized in a small-ish region close to the crack tip.
0.25
0
Atomic stress (σyy) eV/Å3

## Slide 14: Another example of high-throughput large scale simulations: calibration of damping boundaries
Düsseldorf - pyiron hackathon 2024
Tara
2000 Å
1200 Å
0.1
0
Velocity magnitude
Box edge
St-90
St-80
St-70

## Slide 15: Strategy
Düsseldorf - pyiron hackathon 2024
Tara
HPC jobs
Loading large configurations for post-processing, visualization
Visualization in notebook
FAIR